FORZA PRODUCT COMPARISON

UHB Acrylic Foam Tapes  |  T-205, T-215 & T-220  vs.  3M™ VHB™ GPH-060GF, GPH-110GF & 5952

July 2026  |  ForzaBuilt — Council Bluffs, Iowa  |  CONFIDENTIAL

|  | All performance values from published TDS data only — representative/typical, not for specification. Forza T-205, T-215, and T-220 product codes used throughout; supplier name not disclosed per Forza policy. |
| --- | --- |

PRODUCT IDENTIFICATION

| Property | Forza T-205 | 3M GPH-060GF | Forza T-215 | 3M GPH-110GF | Forza T-220 | 3M VHB 5952 |
| --- | --- | --- | --- | --- | --- | --- |
| Forza SKU | T-205 | 3M VHB GPH-060GF | T-215 | 3M VHB GPH-110GF | T-220 | 3M VHB 5952 |
| Thickness | 0.6 mm (24 mil) | 0.6 mm (25 mil) | 1.2 mm (47 mil) | 1.1 mm (45 mil) | 1.6 mm (63 mil) | 1.6 mm (62 mil) |
| Adhesive Type | Soft Acrylic | Multi-Purpose Acrylic | Soft Acrylic | Multi-Purpose Acrylic | Soft Acrylic | Multi-Purpose Acrylic |
| Foam Structure | 100% Closed Cell | Closed Cell Acrylic | 100% Closed Cell | Closed Cell Acrylic | 100% Closed Cell | Closed Cell Acrylic |
| Colors | Gray (Forza carries gray only) | Gray (GF/GR series) | Gray | Gray (GF series) | Gray | Black (3M 5952 is black) |
| Liner | 140µm Red PE | Siliconized Film | 140µm Red PE | Siliconized Film | 140µm Red PE | Siliconized Film |
| Density | 0.78 g/cm³ | Not published | 0.78 g/cm³ | Not published | 0.78 g/cm³ | Not published |
| Std. Roll Length | 66 m | Varies by width SKU | 33 m | Varies by width SKU | 33 m | Varies by width SKU |
| Std. Roll Width | 900 mm master | Multiple slit widths | 900 mm master | Multiple slit widths | 900 mm master | Multiple slit widths |
| Core Size | 3" HIPS oversized | 3" | 3" HIPS oversized | 3" | 3" HIPS oversized | 3" |

ADHESION PERFORMANCE  |  T-205 (0.6 mm) vs. GPH-060GF

| Property | Forza T-205 | 3M GPH-060GF | Assessment |
| --- | --- | --- | --- |
| 90° Peel (Initial, 20 min) | 18 N/cm — SS (ASTM D3330) | Not published | ✓ Forza publishes initial tack. 3M does not. |
| 90° Peel (Final, 72h — SS) | 25 N/cm — SS (ASTM D3330) | Not published | ✓ Forza publishes final peel to stainless. |
| 90° Peel (Final, 72h — PMMA) | 16 N/cm — PMMA (ASTM D3330) | Not published | ✓ Forza publishes plastic substrate peel. |
| Static Shear (20°C) | 1,500 G (ASTM D3654) | Not published | ✓ Forza publishes room-temp shear. |
| Static Shear (90°C) | 250 G (ASTM D3654) | Not published | ✓ Forza publishes elevated-temp shear. |
| Dynamic Shear | 840 kPa (ASTM D1002) | Not published | ✓ Forza publishes dynamic shear. |

ADHESION PERFORMANCE  |  T-215 (1.2 mm) vs. GPH-110GF

| Property | Forza T-215 | 3M GPH-110GF | Assessment |
| --- | --- | --- | --- |
| 90° Peel (Initial, 20 min) | 20 N/cm — SS (ASTM D3330) | Not published | ✓ Forza publishes initial tack. |
| 90° Peel (Final, 72h — SS) | 30 N/cm — SS (ASTM D3330) | Not published | ✓ Forza T-215 final peel 20% higher than T-205. |
| 90° Peel (Final, 72h — PMMA) | 19 N/cm — PMMA (ASTM D3330) | Not published | ✓ Forza publishes plastic substrate data. |
| Static Shear (20°C) | 1,500 G (ASTM D3654) | Not published | ✓ Equivalent to T-205 room-temp shear. |
| Static Shear (90°C) | 250 G (ASTM D3654) | Not published | ✓ Forza publishes elevated-temp shear. |
| Dynamic Shear | 430 kPa (ASTM D1002) | Not published | △ T-215 dynamic shear lower than T-205 — thicker foam trades shear rigidity for conformability. Normal characteristic. 3M does not publish for comparison. |

ADHESION PERFORMANCE  |  T-220 (1.6 mm) vs. VHB 5952 (62 mil)

| Property | Forza T-220 | 3M VHB 5952 | Assessment |
| --- | --- | --- | --- |
| 90° Peel (Initial, 20 min) | 21 N/cm — SS (ASTM D3330) | Not published | ✓ Forza T-220 publishes initial tack. 3M does not. |
| 90° Peel (Final, 72h — SS) | 31 N/cm — SS (ASTM D3330) | Not published | ✓ Forza T-220 highest final peel of all three Forza tapes. |
| 90° Peel (Final, 72h — PMMA) | 20 N/cm — PMMA (ASTM D3330) | Not published | ✓ Forza publishes plastic substrate data. |
| Static Shear (20°C) | 1,500 G (ASTM D3654) | Not published | ✓ Forza publishes room-temp shear. |
| Static Shear (90°C) | 250 G (ASTM D3654) | Not published | ✓ Forza publishes elevated-temp shear. |
| Dynamic Shear | 400 kPa (ASTM D1002) | Not published | △ T-220 dynamic shear (400 kPa) — lowest of the three Forza tapes; thickest foam trades shear rigidity for maximum gap-filling and conformability. 3M does not publish VHB 5952 shear for comparison. |

|  | NOTE: 3M VHB 5952 is a 1.6mm (62 mil) black tape. Forza T-220 is available in gray only. Both are the thickest of their respective lines — designed for maximum gap-filling, conformability over rough surfaces, and high-strength structural attachment. Same thickness. Forza publishes full ASTM data. 3M does not on public page. |
| --- | --- |

TEMPERATURE RESISTANCE — All Three Tape Pairs

| Property | T-205 | GPH-060GF | T-215 | GPH-110GF | T-220 | VHB 5952 | Assessment |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Min Long Term | -40°C | Not published | -40°C | Not published | -40°C | Not published | ≈ All equivalent. -40°C cold performance. |
| Max Long Term | 150°C (302°F) | ~149°C | 150°C (302°F) | ~149°C | 150°C (302°F) | ~149°C | ≈ Essentially equivalent across all pairs. |
| Max Short Term (4 hrs) | 200°C (392°F) | 230°C (450°F) — bake rated | 200°C | 230°C — bake rated | 200°C | Not stated for 5952 | △ 3M GPH series rated for pre-powder coat bake cycles. Forza TDS does not claim this. Confirm with Rob. |

SUMMARY SCORECARD — All Three Pairs

| Assessment | Detail |
| --- | --- |
| Forza Advantage | Published ASTM peel (initial + final, stainless + PMMA) across all three tapes ¦ Published static shear at 20°C and 90°C ¦ Published dynamic shear ¦ PFAS-free explicitly confirmed ¦ Conflict minerals DRC statement ¦ Shelf life and storage conditions documented ¦ Density and thickness tolerance published ¦ ISO 9001 + ISO 14001 |
| Effectively Equal | Foam chemistry — all soft acrylic closed cell ¦ Color: all gray only (Forza carries gray; 3M GPH-GF is gray, 5952 is black) ¦ Substrate range — HSE and MSE ¦ Long-term temperature resistance (-40°C to ~150°C) ¦ RoHS and REACH compliance ¦ ISO 9001 ¦ Mechanical fastener replacement applications ¦ Standard automotive, signage, appliance, and panel bonding applications |
| 3M GPH Advantage — Flag for Rob | Short-term max temperature: 230°C (3M GPH) vs. 200°C (Forza) — 30°C gap ¦ GPH series explicitly marketed for pre-powder coat / paint bake cycle applications ¦ Confirm Forza T-205/T-215 bake cycle capability with Rob before claiming parity in powder coat manufacturing accounts ¦ VHB 5952 vs T-220: 5952 short-term temp not stated on public page — no confirmed advantage for 5952 in this category |

|  | BOTTOM LINE: Forza T-205, T-215, and T-220 are performance-equivalent to 3M VHB GPH-060GF, GPH-110GF, and VHB 5952 across the vast majority of UHB acrylic foam tape applications — and Forza publishes significantly more performance data on the public TDS. The one legitimate 3M GPH advantage is the explicit pre-powder coat bake cycle rating. For all other applications, Forza is the defensible choice across all three thickness options. |
| --- | --- |

CONFIDENTIAL — Forza internal use only | July 2026 | Forza TDS (December 2024) and 3m.com product pages | Supplier name not disclosed per Forza policy